## Slide 1
Paint
Paint
Paint
Paint
Paint
Paint
Paint
Paint
Paint

## Slide 2
Pigments
coloring matter
pigments/dyes
Binders
oils, resin etc.
binds the pigments together
Solvent/Thinner
to adjust paint consistency
Additives
pigment stability, antifreeze, control foaming/skinning
Fillers
color neutral, opaque
Putty
achieving smoothness
ranbsingh

## Slide 3
Paint manufacturing process (schematic)

## Slide 4
an
un-cross-linked
polymer
a highly
cross-linked
polymer
Automobile paint
formulations
Acrylic Lacquers : have
long chains with few, if any,
chemical bond acting as
cross links. When heated
become soft and more
or less fluid
soluble in acetone
Acrylic Enamels : when heated
form an extensively cross-linked
network that becomes extremely
hard and resistant to solvents
Alkyd Enamels : also produce
an extensively cross-linked
surface when heated

## Slide 6
Collection, preservation and packing
Paint evidence is frequently encountered in hit-and
run, burglaries, art forgeries, and occasionally in
other types of offences.
In hit-and run cases, paint may be transferred to
clothing of victims/any other object/the ground
near the point of impact
All the areas are examined, with particular attention
being paid to areas showing pressure effects (glaze
etc), tears, or other contact.

## Slide 7
If paint is found on the garment, it should not be removed; the garment should be marked, carefully wrapped by rolling it in paper and sent it to the laboratory. Such paint will at least show the color of relevant part of the responsible car.
Sometimes whole chips of paint will be transferred to the clothing. If these flakes contain several layers, and in particular if they come from a repainted car then such evidence may have great value when the responsible vehicle is located.
Chips of paint may also be found on the ground near the point of impact in some cases.

## Slide 8
Samples for comparison should be obtained from all areas showing fresh damage on suspected vehicles. This is very important since the paint may be different in type or composition in different areas, even if the color is the same.
If bending the metal slightly can flake off the paint, it should be removed in this manner.
If not, the paint should be scraped or chipped off, using a clean knife blade. The blade should be wiped carefully, before collecting each sample. All layers down to the metal should be collected. Each sample should be placed in a separate container.
Cross transfers of paint commonly occur in hit and-run cases of two or more vehicles.

## Slide 9
Loose paint chips should be removed and
wrapped in paper.
If the transfers are smeared on the surfaces,
flake off chips or scrape paint from the vehicle,
including the transferred paint, as well as the top
layer of paint originally on the car.
All of these transfers recovered from different
areas should be kept in separate containers.
The samples should not be placed directly into
envelopes. Most envelopes have unsealed
corners.

## Slide 10
In case of cross transfers, uncontaminated samples
should always be collected from each vehicle from
areas immediately adjacent to each transfer collected.
This is of great importance, since such specimens
permit the laboratory to distinguish between the
transferred paint and the paint originally present on
the vehicle.
Tools used to gain entry into building, safes, or other
places in burglary cases, often contain traces of paint,
as well as other substances, such as plastic, safe
insulation, etc.
Care must be taken that such traces are not lost.
If such transfers may be present, the end of the tool
containing the material should be wrapped in clean
paper and sealed with tape to prevent loss.

## Slide 11
Attempts should never be made to set/fit the tool into marks or impressions found. If this is done, transfers of paint or material can occur and any traces found later will have no significance as evidence.
Specimens of paint should be collected from all areas that the tools may have contacted at the crime scene. These samples should include all layers present.
One should be very careful not to destroy the tool mark in collecting the paint. If possible, one should cut out around the mark, and send it to the laboratory.

## Slide 12
The tool itself may contain paint or other coatings, tracings of which may be left at the crime scene. A careful search should be made for such transfers, particularly in each tool mark.
All the paint samples should be kept in separate containers.
Paint samples should never be kept directly into envelopes unless large pieces are enclosed. Most envelopes have unsealed cracks in the corners and loss or contamination can occur.

## Slide 13
Examination of paint samples
Macroscopic/microscopic examination
Fluorescence/polarizing microscopy
UV-Vis Spectrophotometry
Solvent/microchemical tests
Thin layer chromatography
Pyrolysis gas chromatography (PyGC)
IR Spectrophotometry
Elemental analysis
X-ray diffraction
Physical matching, layer structure, color arrangement, weathering effect etc
for crystalline compounds
ranbsingh

## Slide 16
Technique for preparing thin sections

## Slide 17
50 finishing coat, 10 under coat
5 primer (chance : 1 in 2500)
6 or more layers reveal source
correspondence
ranbsingh

## Slide 18
Two coat metallic
top coat (burgundy red)
3-µ thin section
Red organic pigments
Solid line – red 179
Broken line red 122
UV –visible absorption spectra

## Slide 19
UV –visible absorption spectra
three vehicles painted with metallic paint carnelian red
all the three base coats are clearly differentiated because of pigment differences in batches

## Slide 20
Pyrolysis gas chromatography
is an invaluable technique for
distinguishing most of the
paint formulations.
Paint chips as small as 20
micrograms are decomposed
by heat into numerous
gaseous products.
Pyrograms of acrylic enamel
paints removed from two
different vehicles

## Slide 21
DERIVATISATION
Pyrograms of pentaerythritol ortho-phthalic alkyd resin Paint
obtained by
packed column PyGC,
capillary column PyGC, and
Thermal assisted Hydrolysis
and Methylation GC
MA methacrolein, C6LA hexanal, C8AL octanal, PA phthalic anhydride, etc. etc.

## Slide 22
Pyrogram of four acrylic latex architectural paints having different monomer compositions
MMA methylmethacrylate
BA butylacrylate
S styrene
EA ethylacrylate
EHA 2-ethylhexylacrylate
etc. etc.

## Slide 23
Pyrogram of two acrylic enamel automobile original topcoat finishes by PyGC/MS
MMA methylmethacrylate
BuOH n-butanol
BMA butylmethacrylate
HPMA hydroxypropylmethacrylate
etc, etc.

## Slide 24
THM profile of the baked alkyd enamel
paint smear found on a baseball bat
found to be consistent with
the paint from a Honda vehicle

## Slide 25
THM-GC-MS Pyrogram
polyester automotive body filler

## Slide 26
Diamonds with sample
Low-pressure diamond cell

## Slide 30
Effects of the cutoff wavelength of KBr and CsI optics on the inorganic data observed in the lower IR region

## Slide 31
Infrared spectra of
automobile topcoats
(inorganic pigments)
A Molybdate orange
B a red enamel, which
contains Molybdate orange
C an orange-brown enamel,
which contains ferric oxide
and Molybdate orange
D a red-brown enamel,
which contains ferric oxide
and Molybdate orange

## Slide 32
IR spectrum of a melamine formaldehyde-modified alkyd resin

## Slide 33
IR spectrum of an acrylic resin

## Slide 34
IR spectrum of an epoxy resin

## Slide 35
IR spectrum of nitrocellulose resin

## Slide 36
IR spectrum of polyvinyl acetate

## Slide 37
IR spectrum of titanium dioxide (TiO2 rutile)

## Slide 38
IR spectrum of talc (3MgO.4SiO2.H2O)

## Slide 39
IR spectrum of kaolin (Al2O3.2SiO2.2H2O)

## Slide 40
IR spectrum of barium sulphate (BaSO4)

## Slide 41
IR spectrum of unknown paint sample

## Slide 42
IR spectrum of the alkyd resin component of unknown paint sample
(in the previous projection)

## Slide 43
IR spectrum of a white acrylic melamine original automotive paint LC81AO466 (NBS)
Pyrolysis gas chromatogram of a white acrylic melamine original automotive paint LC81AO466 (NBS)
notice the presence of peak at retention time 8.55 minute

## Slide 44
IR spectrum of a white acrylic melamine original automotive paint DC81AO466 (NBS)
Pyrolysis gas chromatogram of a white acrylic melamine original automotive paint DC81AO466 (NBS)
notice the absence of peak at retention time 8.55 minute

## Slide 45
IR spectrum of a white alkyd automotive refinish paint (Canadian Industries Ltd.)
Pyrolysis gas chromatogram of a white alkyd automotive refinish paint (Canadian Industries Ltd.)
notice presence of urate absorptions at 1680 and 1520 cm-1

## Slide 46
IR spectrum of a white alkyd automotive refinish paint (Nason)
Pyrolysis gas chromatogram of a white alkyd automotive refinish paint (Nason)
notice absence of urate absorptions at 1680 and 1520 cm-1

## Slide 50
Stair-step carving of a three layer paint chip

## Slide 51
Spectrochemical analysis of paint samples
a
b
a-control; b-from the accident site
the two spectra match line by line, which shows that the sample a and
b have same elemental composition

## Slide 52
COCCOLITHS from PUTTYY
Coccoliths are the skeletons of micro-organisms which lived in the ancient seas from which chalk was deposited.
They differ in appearance according to the precise geological horizon from which the
chalk used in the putty was quarried