## Slide 1
Examination of
wires and cables
ranbsingh

## Slide 2
ranbsingh
Objects (material)
Natural
* major and minor constituents
controlled by nature (within specific range)
* trace constituents vary at random
* change with time (environment, source etc.)
Manufactured
* major and minor constituents
controlled by manufacturer (within specific range)
* trace constituents vary at random
* bulk production and wide distribution

## Slide 3
Ingot
Wire bars
Rolled wire rods
Hard drawn wire
Rod A
Rod B
known
obscure
known

## Slide 4
Examination of wires
Measurement of gauge(diameter)
physical match of cut ends
die marks on the surface
material
electrical resistance
trace element profile
ranbsingh
(class/individual characteristics)
(individual characteristics)
(individual characteristics)
(class characteristics)
(class characteristics)
(class characteristics)

## Slide 5
ranbsingh
Telegraph wires
2.43 - 2.53 mm
2.77 - 2.87 mm
3.42 - 3.52 mm
Measurement of diameter
Diameter should be measured in mutually perpendicular directions at a place
Readings should be taken at least, at
three places on a sample
Average of the above six readings should be
taken for comparison

## Slide 6
physical match of cut ends

## Slide 7
Comparison of striations (die marks) on the surface of wires

## Slide 8
Forensic
Trace element analysis
 Determination of a specific element
(for example, Contact transfers)
 Determination of a group of elements
(for example, gun shot residue)
 Trace element profiling for characterization
(for example: metallic wire, opium)
 Common contaminants in known and
questioned samples
major constituents 10 - 100 percent
trace constituents 1 - 100 ppm
ultra trace constituents .001 - 1 ppm
ultra-ultra trace constituents less than .001 ppm
Levels of constituents
minor constituents .1 - 10 percent

## Slide 9
Composition Of Bauxite
Moisture
L O I
Al O
2
3
Fe O
2
3
TiO
2
SiO
2
V O
2
5
P O
2
5
CaO
1.0
22.3
51.3
14.1
8.0
3.0
0.2
0.19
0.08
Cr O
2
3
MgO
MnO
2
ZrO
2
ZnO
Ga O
2
3
BeO
Specific
gravity
0.07
0.03
0.02
0.10
0.01
0.008
0.001
2.8
ranbsingh

## Slide 10
Impurities detected in aluminum
B
Cr
Cu
Fe
Pb
Mg
Mn
Ni
Ti
V
5
22
7
7
14
21
7
7
12
15
Mn
Cu
Ga
La
Sm
Cr
Fe
Hf
Sc
2.5
6.5
4.5
11
12.5
1.8
3.5
10
6.5
spectrographic analysis
neutron activation analysis
elements
analyzed
coefficient of variation(%)
elements
recommended for
characterization
analyzed
elements
recommended for
elements
characterization
Mn, Cr, Hf, Sc, Fe
Tagging: silver
coefficient of variation(%)
Titanium
Samarium
Scandium
Silicon
Sodium
Potassium
Tin
Vanadium
Ytterbium
Zinc
Zirconium
Manganese
Nickel
Magnesium
Lutetium
Iron
Lanthanum
Lead
Hafnium
Chromium
Cobalt
Copper
Cerium
Beryllium
Boron
Bismuth
Arsenic
Antimony
Calcium
Gallium
Phosphorous
Ni, Cr, B, Mn, Fe
in order of discrimination potential
in order of discrimination potential
ranbsingh

## Slide 11
Trace element profile of copper
Impurities detected
(NAA OES)
and
Antimony
Cobalt
Iridium
Nickel
Tellurium
Arsenic
Gold
Lead
Silver
Tin
Bismuth
Iron
Manganese
Selenium
Zinc
elements recommended for
characterization
Ag, Se, Sb, Au
Neutron activation analysis
ranbsingh

## Slide 12
Fifty six samples
from a hundred meter copper wire
Elements Ag Se Sb Au
Mean concentration 12.7 4.3 4.0 0.6
(value in ppm)
Coefficient of 3.5 4.2 2.2 3.8
variation(%)
ranbsingh

## Slide 13
Comparison of copper wires
Case A
concentration in ppm
Ag Au Sb Se
questioned
known
known
Case B
questioned
known
known
14.0 0.51 7.0 2.7
0.2 0.03 2.2 0.7
0.3 0.03 2.1 0.7
14.0 0.52 7.0 2.7
7.9 0.06 0.5 4.5
14.0 0.52 7.0 2.7
could not be
distinguished
on the basis
of physical,
chemical,
and electrical
properties
*
*
*

## Slide 14
Strands of different Cables having
similar impurity levels
Ag
Au
Sb
Se
B2
10.4
0.074
4.4
0.8
C17
10.1
0.074
4.0
0.8
Average values of impurity levels
in three different multi-stranded cables
C
11.97
0.0458
2.237
0.68
B
11.76
0.0464
2.413
0.65
A
10.25
0.0628
0.302
1.47
Ag
Au
Sb
Se

## Slide 15
Different Strands of the same Cable having
indistinguishable impurity levels
Ag
Au
Sb
Se
A2
12.5
0.018
0.20
0.6
A3
12.3
0.017
0.22
0.6
A9
10.9
0.017
0.18
0.5
A10
11.0
0.019
0.19
0.5
B3
7.6
0.005
0.10
0.4
B9
7.6
0.004
0.08
0.3
B19
7.8
0.006
0.08
0.3
C14
12.1
0.011
0.13
0.5
C15
12.1
0.012
0.13
0.4

## Slide 16
Physical correspondence of strands

## Slide 17
Wire links transmitter with suspect terrorist
two pairs of flex from the transmitter A1, A2 & B1, B2
two pairs of flex from the suspect C1, C2 & D1, D2
Each had seven strands; 3-iron strands & 4-copper strands
Diameter of each strand was 0.27 mm
All the strands were marked sequentially and analyzed
Neutron Activation Analysis technique was used
Flexes could be grouped into; (1) A1, B1, C2, D2 and (2) A2, B2, C1, D1
The suspect was associated with the transmitter

## Slide 22
1977
A priori assumptions
-within agreement,
-between variations
were verified
Forty five inter-comparisons
were made, and it was shown
that the levels of the elements:
Ag, Au, Se, and Sb could
differentiate all the wires
The above method was used
to analyze and report on case
samples with confidence
1997
Trace element profile of
one hundred and eleven
copper wires from actual cases were compiled
Six thousand one hundred
and five inter-comparisons
were made. The wires could
be grouped into one hundred
different sources only
If indistinguishable samples were not
duplicates, the confidence in forming
opinion is affected. Determination of
a few more elements may be essential
ranbsingh
Characterization of
(Neutron Activation Analysis)
Copper Wires by Trace Element profile

## Slide 23
Characterization of Wires by their
Trace Element Profile
is it a
Definitive Identification Technique
Multi-stranded Cables
comparison of trace element concentration in
corresponding strands yields conclusive results
(beyond reasonable doubts)
Wire (single strand)
- indistinguishable (highly consistent with)
- distinguishable (mismatch)

## Slide 24
Characterization of Metals by their
Trace Element Profile
Whether
Different Databases on Trace Impurities
can be Shared
Accuracy
- closeness of the measured value
to the true value
Systematic error in
measurements (bias)
- difference between measured
and true values
Standard deviation
- an index of precision
* Validation of analytical technique
Generation of Analytical data of Known Quality
* Quality Assurance Measures